## Slide 1: microscopic effects in the manipulation of hole spin qubits and hybrid devices
JOSÉ CARLOS ABADILLO-URIEL
ICMM-CSIC
jc.abadillo.uriel@csic.es

## Slide 2: outline
1. Intro: hole spin qubits
2. Manipulation mechanisms
3. spin-photon interactions
4. hybrid super-semi devices with holes
5. conclusion

## Slide 3: Introduction
From Chatterjee et al., Nature Reviews Physics, 3, 157-177 (2021)
Transmons are leading the race: IBM’s 1121 qubits
Si and Ge QDs are particularly promising for quantum computing purposes

## Slide 4: Why semiconductors?
Industrially compatible
Good coherence times & gate manipulability
Prospects of scalability (small unit cell)
High-temperature operation (4K)
From Petit et al., Nature 580, 355-359 (2020)
From Chatterjee et al., Nature Reviews Physics, 3, 157-177 (2021)

## Slide 5
Basic operation of qd qubits
  Electrons/holes are confined in a quantum well
  The electron/hole is pushed against the interface
  Gates are used to manipulate the qubits
  Readout: spin-to-charge conversión
  Original implementations in GaAs/AlGaAs heterostructures

## Slide 6: status
-High single-qubit gate fidelities have been demonstrated. See
Nature Nanotechnology 13, 102-106 (2018)
Nature volume 569, pages 532–536 (2019)
Nature Communications volume 11, Article number: 4144 (2020)
-Two-qubit gates beyond QEC threshold. See
Nature 601, 343-347 (2022)
-Working six-qubit processor with electrons
Nature 609, 919–924 (2022)
Nature 591, 580–585 (2021)
12-qubit processor from Intel (not many details yet)
-4K operation demonstrated
Nature 580, 355-359 (2020)

## Slide 7: Why hole spin qubits are cool?
Qubit properties are highly tunable through gate voltages
Cool physics: anisotropic g-matrices, Rashba SOC, sweet spots
High SOC : fast all-electrical manipulation
mJ=±1/2
mJ=±3/2
J=3/2
Partial insensitivity to hyperfine noise

## Slide 8: High-Fidelity operation has been achievied
    Hendrickx et al., Nature 591, 580–585 (2021)
  State of the art
  4-qubit processor: single-qubit gates above 99.9% and
  two-qubit above 99% (Hendrickx et al., Nature 591, 580–585 (2021))
  Ongoing experiments with 10 qubit device
  Large coherence T2*~90 μs (Piot et al., Nat. Nano (2022))
  “Hot”-qubit operation ~ 4K (Carmenzind et al., Nat. Electronics 5, 178–183 (2022))
  Spin-photon coupling of 330 MHz in hybrid Si-cQED system (Yu et al., Nature Nanotechnology (2023))

## Slide 9: 2. understanding manipulation mechanisms
-In the experiments the hole is driven laterally, in parallel to an in-plane magnetic field
for holes in Ge, g_x ~ g_y ~ 0.05-0.6 g_z ~ 13.5
-Hamiltonian of a hole under a magnetic field
-We perform simulations on planar dots (isotropic in-plane confinement)
    Hendrickx et al., Nature 591, 580–585 (2021)

## Slide 10: Thanks to my collaborators
Esteban Rodríguez
Biel Martínez
Yann-Michel Niquet

## Slide 11: First suspect: rashba soc
-Lack of inversion symmetry. Determined by geometry and gates
Requires strong fields (hard for Ge/GeSi)
Michal et al., Phys. Rev. B 103, 045305 (2021)
Bosco et al., Phys. Rev. B 104, 115425 (2021)
-Nanowire or anisotropic dots (linear Rashba).
See Golovach et al. (2006) PRB 74
-Planar isotropic dots (cubic Rashba)
More effective when magnetic field is vertical Bz

## Slide 12: Second suspect: g-tmr
-g-factor is anisotropic. By driving g-tensor the hole feels a time-dependent magnetic field
-Deforming the dot with electric fields induces changes in the g-tensor
Effective when
Crippa et al. (2018) PRL 120
Kato et al. (2003) Science 229
qxz
g(V(t))

## Slide 13
In the experiment, they use in-plane magnetic fields which are inefficient for both cubic Rashba and gTMR
Is there some missing mechanism?
Cubic rashba and gtmr are not fully consistent with experiments
Reviewing some assumptions:
-Separable electric fields
-Homogeneous strain

## Slide 14
How we simulate
-Poisson solver for realistic electrostatics as functions of gate voltages
-Numerical solution to Kohn-Luttinger Hamiltonian
-g-matrix formalism to extract Rabi frequencies for given magnetic field orientations

## Slide 15
INHOMOGENEOUS & NON-SEPARABLE CONFINEMENT FIELDS
Gates have finite size and are separated a certain distance away from the hole

## Slide 16: We can capture the physics with a non separable potential
The effective Hamiltonian for GS heavy-hole subspace can be obtained through Schrieffer-Wolff transformation. The subbands couple through
Physically, it is similar to a gTMR mechanism
When the potential is separable

## Slide 17
Non-separable field allows in-plane manipulation
x
y
z
Cubic Rashba
Non-separable feature
Still, Rabi frequencies are low. What’s missing?

## Slide 18
adding INHOMOGENEOUS STRAIn
Device is made with different materials with different expansion coefficients
Strain is assumed to be biaxial due to barrier & well lattice mismatch
Experiments had shown rotations in the g-matrix consistent with residual strains
Liles et al., Phys. Rev. B 104, 235303 (2021)
Piot et al., Nat. Nano (2022)

## Slide 19
Numerically minimizing the elastic energy density at low T, leads to inhomogeneities commensurate with the gate stack
Inhomogeneous strains are ubiquitous

## Slide 20
Inhomogeneous strains induce magnetic gradients
At equilibrium
Strain corrections to g-matrix

## Slide 21
STRAIN INDUCES NEW GTMR AND RASHBA MECHANISMS
x
y
z
Linearized Rashba
Enhanced in-plane feature
Rabi frequencies now are much larger: strain dominates

## Slide 22
STRAIN slightly improves quality factors
In-plane sweet spot
Out-of-plane quasi-sweet spot

## Slide 23
Rabi freq. dependence with thicknesses

## Slide 24
Interfaces also lead to linear rashba and Dresselhaus terms
We perform TB simulations to characterize the spin-splitting of the first HH band in Ge/GeSi heterostructures
The symmetry reduction from Oh to C2v leads to allowed Rashba and Dresselhaus terms
Rashba term is related to an interaction between conduction and valence bands

## Slide 25
Interface Terms lead to corrections to g-factors and rabi freqs
Ivchenko et al., Phys. Rev. B 54, 5852 (1996)
SW
The Dresselhaus interaction leads to a small in-plane rotation of the g-factors, which in turn skews slightly the Rabi freqs
We note that disordered interfaces tend to kill this effect

## Slide 26
Take-home part 1
We found that non-separable field and inhomogeneous strains lead to new manipulation mechanisms
Optimal operation with in-plane magnetic fields for fixed Larmor frequency
Strain-mediated mechanisms dominate hole manipulation

## Slide 29: 3. Spin-photon coupling
Dijkema et al., arXiv: 2310.16805
Interaction distance
Mills et al., Nat. Comm. 10 (2019)
Charge shuttling in a QD array
Photon mediated interaction
Nearest neighbor exchange interaction
Veldhorst et al., Nature 526 (2015)
  Jadot et al., Nat. Nano. 16, 570–575 (2021)

## Slide 30: Electron-photon interfaces in Si
Mi et al.
Nature 555, 590 (2018)
Samkharadze et al.
Science 359, 1123 (2018)
Photons couple readily to the charge of the electron
To couple the spin to the photon one needs to induce an artificial SOC: micromagnets
Coupling in the tens MHz
Decoherence rates in few MHz

## Slide 31
What if we take advantage of the intrinsic
SOC of holes?
Phys. Rev. B 107, L041303 (2023)
Nature Nano. 18, 741-746 (2023)

## Slide 32: Thanks to my collaborators
Vincent Michal
Michele Filippone
Yann-Michel Niquet
Cecile Yu
Simon Zihlmann
Romain Maurand

## Slide 33
Exploring the minimal setup in si nanowires
-Hole SOC allows minimal setup coupling to
quantized fields
-Thin dot limit with strong y field
-See Bosco PRL 129, 066801 (2022)
for setups based on Rashba driving
Phys. Rev. B 107, L041303 (2023)

## Slide 34
Anisotropic response: transverse and longitudinal
|
|

## Slide 35
Transverse and longitudinal couplings
Reciprocity between transverse and longitudinal coupling:
Reciprocal sweetness
Arxiv:2412.13069

## Slide 36
high-fidelity operation is achievable at the ss
Quantum state transfer: exchange between photonic and spin excitations
High-fidelity operation is feasible with longitudinal coupling using curvature driving

## Slide 37: Experiment: Circuit QED with hole spins in Si
NbN CPW resonator , GHz
Co-fabrication with resonator at interconnect layer (M1), connected by W vias
Si nanowire transistor on SOI with one gate connected to the resonator
GHz
13.5 MHz
MHz
MHz
Nature Nano. 18, 741-746 (2023)

## Slide 38: Circuit QED with hole spins in Si
Nature Nano. 18, 741-746 (2023)

## Slide 39: Charge-photon interaction
MHz
GHz
Cavity response to a probe field

## Slide 40: Strong spin-photon coupling
Strong spin-photon coupling with MHz MHz
Vacuum Rabi mode splitting
 signature of strong coupling

## Slide 41: Strong spin-photon coupling: angular dependence
heavily depends on the magnetic field orientation

## Slide 42: Angular dependence

## Slide 43: Strong spin-photon coupling: angular dependence
maximizes spin-photon coupling
Max cooperativity

## Slide 44: Interplay between Zeeman and SO field
is the length over which there is a spin flip
is the spin-orbit unit vector over which the spin precesses as it moves in x
x
z
y
Tunneling flips the spin
Tunneling preserves the spin
In our case:

## Slide 45: Angular dependence of and
g-factors
and for anisotropic g-factors
and for averaged g-factors

## Slide 46: vs –maps: Measurement of and SOI

## Slide 47: Single-dot limit
Michal et al. Phys. Rev. B 107, L041303 (2023)
Bosco et al. PRL 129, 066801 (2022)

## Slide 48: Conclusions part 2
Holes offer new opportunities for spin-photon coupling
Si-MOS hole spins embedded in a high-impedance cavity
Si-MOS hole charge bordering ultra-strong charge-photon coupling with
Unprecedented spin-photon coupling MHz
First demonstration of sizeable coupling in single dot limit MHz
OUTLOOK
Ultrastrong coupling regime theory and two-photon processes
Multidot effects
Missing effects such as inhomogeneous strains

## Slide 49: 4. superconducting proximity effect in hole-based Ge hybrid semi-super devices
D. Míchel Pino
Rubén Seoane Souto
María José Calderón
Ramón Aguado
J. C. Abadillo-Uriel
Arxiv:2501.00088

## Slide 50: Why Hybrid devices & why Ge?
Hybrid super-semi devices. Connectivity + gate-tunability Andreev spin qubits, gatemons
Hays et al., Science 373, 6553 pp. 430-433
InAs Andreev Spin Qubits show limited coherence Pita Vidal et al., Nature Physics 19, 1110-1115 (2023) Hays et al., Science 373, 6553 pp. 430-433
Semiconductor Spin qubits
Superconducting qubits

## Slide 51: Holes as candidates for hybridization
Spin qubit properties are gate-tunable
Unusual forms of SOC :
Strain induced: J.C. Abadillo-Uriel et al., PRL 131, 097002 (2023) Linear Rashba: Michal et al., Phys. Rev. B 103, 045305 (2021)
Bosco et al., Phys. Rev. B 104, 115425 (2021) Inseparable electric effects: B. Martínez, J.C. Abadillo Uriel, et al., PRB 106, 235426 (2022)
Question is then: what happens if we add superconductivity to the mix?
First super-Ge devices show a large induced gap ~60 meV Lakic et al., Nat. Materials (2025); Tosato et al., Nat Comms 4 23 (2023); Sagi et al., Nat Comms 15, 6400 (2024).

## Slide 52: Comprehensive study of the proximity effect

## Slide 53: Effective CB pairing effects into the 4kp model

## Slide 54: Full 4kp model for 2DHG

## Slide 55: CB PAIRING EFFECTS IN THE RASHBA BASIS (OR KL BASIS)
Analytical effective Hamiltonian in the eigenbasis of the hole subspace:
We get intra- and inter-band effective pairings (k- and spin-dependent)
Minigaps are gate tunable, anisotropic, and k-dependent

## Slide 56: HH-lh PAIRING EFFECTS IN THE RASHBA BASIS (OR KL BASIS)
Analytical effective Hamiltonian in the eigenbasis of the hole subspace:
We get intra- and inter-band effective pairings (k- and spin-dependent)
For more negative m Fermi-level anticrossings occur at higher k

## Slide 57: MIXED PAIRING EFFECTS IN THE RASHBA BASIS (OR KL BASIS)
Mixed HH-LH pairing terms are allowed for lower symmetry:
Linear-in-k. Quite anisotropic

## Slide 58: PUTTING IT TOGETHER
CB proximity:
Minigaps are gate tunable, anisotropic, and k-dependent (quadratic)
HH & LH proximity:
For more negative m Fermi-level anticrossings occur at higher k
Linear-in-k. Quite anisotropic
Mixed HH-LH proximity:
HHs
LHs

## Slide 59: Induced pairing effects through the bands
CB proximity:
Minigaps are gate tunable, anisotropic, and k-dependent (quadratic)
HHs
LHs

## Slide 60: EFFECT of different bands
CB proximity:
Minigaps are gate tunable, anisotropic, and k-dependent (quadratic)
HH & LH proximity:
For more negative m Fermi-level anticrossings occur at higher k
HHs
LHs

## Slide 61: EFFECT of different bands
CB proximity:
Minigaps are gate tunable, anisotropic, and k-dependent (quadratic)
jc.abadillo.uriel@csic.es
HH & LH proximity:
For more negative m Fermi-level anticrossings occur at higher k
Linear-in-k. Quite anisotropic
Mixed HH-LH proximity:
HHs
LHs

## Slide 62: EFFECT of different bands
CB proximity:
Minigaps are gate tunable, anisotropic, and k-dependent (quadratic)
HH & LH proximity:
For more negative m Fermi-level anticrossings occur at higher k
Linear-in-k. Quite anisotropic
Mixed HH-LH proximity:
HHs
LHs

## Slide 63: Vertical Zeeman: f-wave superconductivity
Geometrical competition between the Rashba spin-splitting and the Zeeman field:
DOS estimation:
The gaps closes with vertical field but it makes the transverse component stronger (f-wave)

## Slide 64: IN-plane Zeeman: GAP VS PAIRING. BOGOSURFACES
Direct vs geometrical competition between the Rashba spin-splitting and the Zeeman field:
If Larmor vector is parallel to the Rashba splitting, the spectrum gets titled

## Slide 65: Rich van hove singularities in dos
Van Hove singularities boil down to minima and maxima in the anisotropic spectral gap

## Slide 66: Rich van hove singularities in dos

## Slide 67: Take-home part 3:
SuperHoles exhibit some exotic superconducting pairing terms
Experimentally measured gaps seem to be mostly direct but may have small mixed and CB contributions
Gaps are strongly anisotropic and have complex competition with B fields
Experimental signatures in DOS: Bogoliubov bands, van Hove singularities

## Slide 68: Conclusions
Holes are interesting creatures with cool physics still being unveiled
New mechanisms for manipulation: inhomogeneous electric fields: Phys. Rev. B 106, 235426 (2022)
inhomogeneous strain: PRL 131, 097002 (2023)
Natural spin-photon coupling: Nature Nano. 18, 741-746 (2023)
Single dot spin-photon architectures are possible: Phys. Rev. B 107, L041303 (2023)
Rich hybrid physics: arxiv:2501.00088

## Slide 69: Characterizing the charge-photon coupling
Dispersive shift at
MHz
GHz